## Slide 1
Incozol-341 LV - Switch Effortlessly. Save Instantly.

## Slide 2: You asked and we listened…….
"We value your product/service and want to make this work—are there any pricing options you could offer?
“The one area where our testing showed a slight downside was the film hardness”
“Is there anything new in the Incozol range?”

## Slide 3: The development of Incozol-341 LV
Incozol LV was developed in the 90s and we know much more about Oxazolidine technology now
The formulation is impacted by ongoing increases in raw material prices
Customer feedback has given us input for development
We proactively updated our manufacturing processes to meet health and safety regulations
Why?

## Slide 4: Introducing Incozol-341 LV
Better performance than Incozol LV
Drop in replacement
Better value

## Slide 5: Summary – 2k pu automotive refinish clearcoat
 | Incozol LV Standard | Incozol-341 LV
Appearance |  | 
Potlife | 40 | 40
1 day hardness |  | 
7 day hardness |  | 
Drying time |  | 
Chemical and Stain Resistance |  | 
Abrasion Resistance |  | 
Scratch resistance (abraded steel) |  | 
Mandrel bend |  | 
Adhesion |  | 
 = Good  = Excellent

## Slide 6: Summary – 2K PU heavy duty white topcoat
 | Incozol LV Standard | Incozol-341 LV
Appearance |  | 
Potlife | 45 | 40
1 day hardness |  | 
7 day hardness |  | 
Drying time |  | 
Chemical and Stain Resistance |  | 
Abrasion Resistance |  | 
Scratch resistance (abraded steel) |  | 
Mandrel bend |  | 
Adhesion |  | 
 = Good  = Excellent

## Slide 7: Formulator-Ready: High-Performance Oxazolidine Innovation Physical properties
Property | Incozol LV | Incozol-341 LV
Viscosity | 55 | 75
Colour (APHA) | Max 250 | Max 250
Equivalent Weight | 86 | 82

## Slide 8
Chart: Polyol Replacement (%)
| 0 | 5 | 10 | 15 | 20
Incozol LV | 7020 | 4560 | 3220 | 2430 | 1745
Incozol-341 LV | 7020 | 4700 | 3140 | 2400 | 1580
#REF! | 1
Dilution curve shows Incozol-341 LV has the same ability to reduce viscosity as Incozol LV

## Slide 9
2k pu automotive refinish Clearcoat

## Slide 10: Guide Formulation Incozol LV 2k pu automotive refinish clearcoat
Part A |  | 
Component |  | Parts by weight / g
Acrylic Polyol | Joncryl 507 | 47.70
UV Absorber | Tinuvin 1130 | 0.30
UV Stabiliser | Tinuvin 292 | 0.30
Flow & Levelling Additive | BYK 399 | 0.50
Solvent | Butyl Acetate | 43.40
Catalyst | TIB KAT 216 (10% Sol in BA) | 0.50
Moisture Scavenger | Incozol 2 | 2.00
Reactive Diluent | Standard Incozol LV/Incozol-341 LV | 5.30
Part B |  | 
Component |  | Parts by weight / g
PolyIsocyanate | Desmodur N3300 | 40.10
The same formulation was used throughout, with the only variable being the reactive diluent
Formulated to the same VOC
A comparison was made between standard Incozol LV and the new Incozol-341 LV

## Slide 11: physical properties
Property | 2K PU Automotive Refinish Clearcoat (Inc LV Std) | 2K PU Automotive Refinish Clearcoat (Incozol-341 LV)
Pot Life (min) | 40 | 40
% Solids | 62.58 | 64.72
Mixed Viscosity (sec) - Ford Cup B4 | 18 | 21
Mixed SG (g/L) | 1.00 | 1.01
2K PU Automotive Refinish Clearcoat with Inc LV Standard
2K PU Automotive Refinish Clearcoat with Incozol-341 LV
Offers comparable physical properties to Incozol LV and can be seamlessly substituted without the need for reformulation
Ask Georgina about Voc And solids

## Slide 12: dry film properties
Property | 2K PU Automotive Refinish Clearcoat (Inc LV Std) | 2K PU Automotive Refinish Clearcoat (Incozol-341 LV)
Gloss @ 60° GU 1d | 198 | 197
Gloss @60° GU 7d | 195 | 194
Persoz Hardness (s) 1d | 77 | 121
Persoz Hardness (s) 7d | 254 | 271
Early hardness development - Improved 1 day and 7 day hardness when compared to Incozol LV

## Slide 13: Faster drying with Incozol-341 LV
Comparable drying time when compared to Incozol LV
Chart: Time in minutes
| Tack free | Hard-dry | Through- dry
Incozol LV | 75 | 150 | 200
Incozol-341 LV | 60 | 135 | 190
15 minutes faster tack-free tie
Improved through dry time
No change in formulation required

## Slide 14: Chemical and stain resistance
Chart: 
| Acetone: Water 1:1 | IPA: Water 1:1 | 1M HCl | 0.1M NaOH | Bleach | Coffee | Red Wine | Detergent | Water Saturated Sponge | Petrol | Brake Fluid | Engine Oil
Inc LV STD | 5 | 5 | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 4 | 5
Incozol-341 LV | 5 | 5 | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 4 | 5
Scoring Key | 0 | film removal | 3 | heavy staining
 | 1 | heavy cracking | 4 | light staining
 | 2 | light cracking | 5 | no change
After 24 hours recovery time only light staining from Brake fluid can be observed.
Same excellent chemical and resistance as formulation with standard Incozol LV

## Slide 15: 2k Taber abrasion test
Incozol LV Standard- after Taber Abrasion
Incozol-341 LV- after Taber Abrasion
Enhanced ability to withstand wear and friction using Incozol-341 LV making it suitable for demanding applications
Chart: 33% improvement in abrasion resistance
| % loss
Incozol LV | 0.26
Incozol 331 | 0.18
*based on reduced material loss in Taber testing (33 mg vs. 47 mg

## Slide 16: Scratch resistance
Pass/Fail | 2K PU Automotive Refinish Clearcoat (Inc LV Std) |  |  |  | 2K PU Automotive Refinish Clearcoat (Incozol-341 LV) |  |  | 
 | Steel |  |  | Aluminum | Steel |  |  | Aluminum
 | Cleaned | Abraded | Not Abraded or Cleaned |  | Cleaned | Abraded | Not Abraded or Cleaned | 
Mark( g) | 200 | 200 | 200 | 100 | 200 | 200 | 200 | 100
Pass (g) | 4000 | 4000 | 4000 | 1100 | 4000 | 4000 | 4000 | 1100
Failed (g) | N/A | N/A | N/A | 1200 | N/A | N/A | N/A | 1200
Maintains the scratch resistance performance of Incozol LV
Method Standard: BS3900 Part 2 - Scratch Resistance (max 4000g weight) : 7 days@room temp
Maintains scratch resistance even on unprepared surfaces
Performs consistently across steel and aluminium
No compromise in performance with Incozol-341 LV

## Slide 17: Same Superior flexibility as Incozol lv
Mandrel Size | 2K PU Automotive Refinish Clearcoat (Inc LV Std) | 2K PU Automotive Refinish Clearcoat (Incozol-341 LV)
2mm | Pass | Pass
6mm | Pass | Pass
Method Standard: ASTM D 522_A: 7 days@room temp
Passes flexibility test at 6mm and 2mm
No cracking or delamination
Change 331 under this picture

## Slide 18
Condition | 2K PU Automotive Refinish Clearcoat (Inc LV Std) | 2K PU Automotive Refinish Clearcoat (Incozol-341 LV)
Cleaned | 4B- 97% | 5B- 100%
Abraded and Cleaned | 5B- 100% | 4B- 99%
Not Abraded or Cleaned | 4B- 96% | 5B- 100%
Adhesion scoring key | 
5B | 0% removed
4B | <5 %removed
3B | 5% to 15% removed
2B | 15% to 35% removed
1B | 35% to 65% removed
0B | >65% removed
Superior adhesion even on non abraded substrate
Method/Standard: ASTM D 3359: 7 days @ room temp
Cross Hatch Adhesion Test (Rank/ Percentage intact)
100% adhesion on unprepared surfaces with Incozol-341 LV
No cracking or delamination
Offers improved impact resistance

## Slide 19: Adhesion Test (Cross Hatch)
Incozol LV Standard
Incozol-341 LV
Incozol LV Standard- Cleaned before tape
Incozol LV Standard- Cleaned after tape
Incozol LV Standard- Abraded before tape
Incozol LV Standard- Abraded after tape
Incozol LV Standard- Not Abraded or Cleaned before tape
Incozol LV Standard- Not Abraded or Cleaned after tape
Incozol-341 LV - Cleaned before tape
Incozol-341 LV - Cleaned after tape
Incozol-341 LV - Abraded before tape
Incozol-341 LV - Abraded after tape
Incozol-341 LV - Not Abraded or Cleaned before tape
Incozol-341 LV - Not Abraded or Cleaned after tape

## Slide 20
2k pu heavy duty white topcoat

## Slide 21: Guide Formulation 2k pu Heavy Duty wHITE Topcoat
Part A |  | 
Component |  | Parts by weight / g
Acrylic Polyol | Joncryl 507 | 40.50
Pigment | Tiona 595 | 17.00
UV Absorber | Tinuvin 1130 | 0.30
UV Stabiliser | Tinuvin 292 | 0.30
Flow & Levelling Additive | Dynoadd F-1 | 0.50
Solvent | Butyl Acetate | 34.4
Catalyst | TIB KAT 216( 10% Sol in BA) | 0.50
Moisture Scavenger | Incozol 2 | 2.00
Reactive Diluent | Standard Incozol LV/Incozol-341 LV | 4.50
Part B |  | 
Component |  | Parts by weight / g
PolyIsocyanate | Desmodur N3300 | 34.6
The same formulation was used throughout, with the only variable being the reactive diluent
A comparison was made between standard Incozol LV and the new Incozol-341 LV
Ask GG about theoretical VOC

## Slide 22: physical properties
Property | 2K PU Heavy Duty White TC (Inc LV Std) | 2K PU Heavy Duty White TC (Incozol-341 LV)
Pot Life (min) | 45 | 40
% Solids | 72.24 | 71.95
Mixed Viscosity (sec) - Ford Cup B4 | 22 | 21
Mixed SG (g/L) | 1.13 | 1.13
Offers comparable physical properties to Incozol LV and can be seamlessly substituted without the need for reformulation
2K PU Heavy Duty White Topcoat with Incozol-341 LV
2K PU Heavy Duty White Topcoat with Standard LV
Ask GG about solids and VOC

## Slide 23: dry film properties
Property | 2K PU Heavy Duty White TC (Inc LV Std) | 2K PU Heavy Duty White TC (Incozol-341 LV)
Gloss @ 60° GU 1d | 96.2 | 96.3
Gloss @60° GU 7d | 96.6 | 95.9
Persoz Hardness (s) 1d | 147 | 166
Persoz Hardness (s) 7d | 272 | 273
Early hardness development - Improved 1 day hardness compared to Incozol LV

## Slide 24
Comparable drying time when compared to Incozol LV
Chart: Time in minutes
| Tack free | Hard-dry | Through- dry
Incozol LV | 150 | 190 | 285
Incozol-341 LV | 150 | 195 | 280
No change in formulation required

## Slide 25: chemical and stain resistance
Chart: 
| Acetone: Water 1:1 | IPA: Water 1:1 | 1M HCl | 0.1M NaOH | Bleach | Coffee | Red Wine | Detergent | Water Saturated Sponge | Petrol | Brake Fluid | Engine Oil
Inc LV STD | 5 | 5 | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 4 | 5
Incozol 331 | 5 | 5 | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 4 | 5
Note that after 24 hours recovery time no staining can be observed.
Same excellent chemical and resistance as standard Incozol LV
Scoring Key | 0 | film removal | 3 | heavy staining
 | 1 | heavy cracking | 4 | light staining
 | 2 | light cracking | 5 | no change

## Slide 26: Taber Abrasion Resistance Test
Incozol LV Standard- after Taber Abrasion
Incozol-341 LV- after Taber Abrasion
Enhanced ability to withstand wear and friction using Incozol-341 LV making it suitable for demanding applications
Below 1% loss is considered to have very high abrasion resistance
Chart: 31% improvement in abrasion resistance
| % loss
Incozol LV | 0.33
Incozol 341 LV | 0.24
Abrasion Resistance (CS-17) (mg/1000 cycles: BS EN ISO7784-2

## Slide 27: scratch resistance
 | Steel |  |  |  |  |  | Aluminium | 
Pass/Fail | 2K PU Heavy Duty White TC (Inc LV Std) |  |  | 2K PU Heavy Duty White TC (Incozol-341 LV) |  |  | 2K PU Heavy Duty White TC (Inc LV Std) | 2K PU Heavy Duty White TC (Incozol-341 LV)
 | Cleaned | Abraded | Not Abraded or Cleaned | Cleaned | Abraded | Not Abraded or Cleaned |  | 
Mark( g) | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100
Pass (g) | 2500 | 2400 | 2500 | 2100 | 2500 | 3000 | 1200 | 1400
Failed (g) | 2600 | 2500 | 2600 | 2200 | 2600 | 3100 | 1300 | 1500
Improved scratch resistance for both steel and aluminum substrates
Improves scratch resistance even on unprepared surfaces
Performs consistently across steel and aluminium
No compromise in performance with Incozol-341 LV

## Slide 28: mandrel bend (flexibility) test
Mandrel Bend Test- Incozol LV Standard (6 mm and 2 mm)
Mandrel Bend Test – Incozol-341 LV (6 mm and 2 mm)
Mandrel Bend (Flexibility) Test |  |  |  |  | 
Test | Method/Standard | Time Period /Conditions | Mandrel Size | 2K PU Heavy Duty White TC (Inc LV Std) | 2K PU Heavy Duty White TC (Incozol-341 LV)
Mandrel Bend Test (Pass/Fail) | ASTM D 522 -A | 7 days @RT | 2 mm | Pass | Pass
 |  |  | 6 mm | Pass | Pass
Excellent ability to withstand deformation without cracking and delaminating

## Slide 29: adhesion test (cross hatch)
Cross Hatch Adhesion Test (Steel) |  |  |  |  | 
Test | Method/Standard | Time Period | Condition | 2K PU Heavy Duty White TC (Inc LV Std) | 2K PU Heavy Duty White TC (Incozol-341 LV)
Cross Hatch Adhesion Test (Rank/ Percentage intact) | ASTM D 3359 | 7 days @RT | Cleaned | 4B- 97% | 5B- 100%
 |  |  | Abraded and Cleaned | 5B- 100% | 4B- 97%
 |  |  | Not Abraded or Cleaned | 2B- 15-35% Affected area | 5B- 100%
Scoring key | 
Rank | % Removed
5B | 0
4B | <5
3B | 5 to 15
2B | 15 to 35
1B | 35 to 65
0B | >65
No loss in adhesion performance using Incozol-341 LV

## Slide 30: Incozol lv tests results
Adhesion Test (Cross Hatch)
Incozol LV Standard
Incozol-341 LV
Incozol LV Standard- Cleaned before tape
Incozol LV Standard- Cleaned before tape
Incozol LV Standard- Abraded before tape
Incozol LV Standard- Abraded after tape
Incozol LV Standard- Not Abraded or Cleaned before tape
Incozol LV Standard- Not Abraded or Cleaned before tape
Incozol-341 LV - Cleaned before tape
Incozol-341 LV - Cleaned after tape
Incozol-341 LV - Abraded before tape
Incozol-341 LV - Abraded after tape
Incozol-341 LV - Not Abraded or Cleaned before tape
Incozol-341 LV - Not Abraded or Cleaned after tape

## Slide 31: Summary – 2k pu automotive refinish clearcoat
 | Incozol LV Standard | Incozol-341 LV
Appearance |  | 
Potlife | 40 | 40
1 day hardness |  | 
7 day hardness |  | 
Drying time |  | 
Chemical and Stain Resistance |  | 
Abrasion Resistance |  | 
Scratch resistance (abraded steel) |  | 
Mandrel bend |  | 
Adhesion |  | 
 = Good  = Excellent

## Slide 32: Summary – 2K PU heavy duty white topcoat
 | Incozol LV Standard | Incozol-341 LV
Appearance |  | 
Potlife | 45 | 40
1 day hardness |  | 
7 day hardness |  | 
Drying time |  | 
Chemical and Stain Resistance |  | 
Abrasion Resistance |  | 
Scratch resistance (abraded steel) |  | 
Mandrel bend |  | 
Adhesion |  | 
 = Good  = Excellent

## Slide 33
Clear Protective Topcoat
Better 1 day hardness
Better scratch resistance
Better adhesion
Incozol-341 LV
Better 7 day hardness
Drop in replacement
Same high performance as Incozol LV
Better value
Switch Effortlessly. Save Instantly.
White Protective Topcoat
Better 1 day hardness
Better scratch resistance
All other properties are the same for both formulas

## Slide 34
Thank you for your attention